## Slide 1: DAB Temperature testing after 2 min. out of the environment chamber at -35 and 85

## Slide 2: Content
Object
Instruments and settings
Result & analysis
Conclusion

## Slide 3: Object
Constant temperature, an key assumption in DAB deployment simulation, has obvious conservative and deviation for cover strength. Therefore, the assumption should be considered cautiously.
Temperature testing has been conducted for analyzing the temperature distribution in four DAB modules. These DAB modules have different structures and materials, whose influence should also be considered.

## Slide 4: DAB Modules
SX12
KC-2
P3011
G95

## Slide 5: DAB Module – SX12 Cover:TES2403 Housing: PG8 PA6 40% fiber Design type: Floating module PE: Maggie Meng

## Slide 6: DAB Module – KC-2 Cover:TES2403 Housing: Steel Design type: Floating module PE: Haojie Gao

## Slide 7: DAB Module – G95 Housing: PG8 PA6 40% fiber Design type: Floating cover PE: Jolay Zhou

## Slide 8: DAB Module – P3011 Cover:TA1081B Housing: Steel Design type: Floating module PE: Kaixuan Zeng

## Slide 9: Instruments and settings
Digital acquisition instrument
Temperature sensor
4 line armoring thermal resistance
Provider: Kecheng Cai
Num.: 1
Channel: 101
K thermal couple (plate)
Provider: Qihe Xiao
Num.: 3
Channel: 103,104,105
K thermal couple (needle)
Provider: P Yigang Sun
Num.: 5
Channel: 106,107,108,109,110
Agilent Digital Acquisition

## Slide 10: Instruments and settings The location of the temperature sensors, testing environment temperature 26~29 ℃, and test time is 2 min.
Channal | Location
101 | DAB center(TR)
103 | Tearline Root(inner)
104 | Cover center(inner)
105 | Cover center(outer)
106 | DAB center(TC)
107 | Inflator Bottom (outer)
108 | Tearline w/o emblem (inner)
109 | Infltor bottom(inner)
110 | Tearline w emblem root(outer)
105
110
107
101 & 106
109
104
108
103
Note: The outer thermal couples (105,110) separated from cover in 85℃.

## Slide 11: Result & analysis SX12
Chart: 
DAB_Center | 82.814 | 82.808 | 82.808 | 82.814 | 82.808 | 82.817 | 82.814 | 82.808 | 82.811 | 82.814 | 82.811 | 82.808 | 82.808 | 82.808 | 82.802 | 82.799 | 82.791 | 82.785 | 82.779 | 82.77 | 82.765 | 82.756 | 82.739 | 82.73 | 82.715
Split line | 82.238 | 82.281 | 82.273 | 82.136 | 81.819 | 81.342 | 80.771 | 80.099 | 79.486 | 78.872 | 78.265 | 77.657 | 77.081 | 76.514 | 75.931 | 75.332 | 74.737 | 74.135 | 73.568 | 73.048 | 72.481 | 71.92 | 71.417 | 70.89 | 70.434
Cover center(inner) | 81.871 | 81.846 | 81.657 | 81.714 | 81.657 | 81.558 | 81.386 | 81.136 | 80.886 | 80.648 | 80.359 | 80.09 | 79.846 | 79.574 | 79.277 | 79.009 | 78.749 | 78.468 | 78.217 | 77.946 | 77.666 | 77.407 | 77.154 | 76.881 | 76.61
Cover center(outer) | 81.775 | 79.036 | 74.201 | 68.897 | 67.244 | 65.998 | 64.484 | 63.208 | 63.116 | 62.896 | 62.965 | 62.628 | 62.281 | 61.92 | 61.536 | 61.429 | 61.517 | 61.392 | 60.57 | 60.154 | 59.379 | 59.35 | 59.352 | 59.549 | 59.6
Chart: 
DAB_Center | -33.552 | -33.551 | -33.552 | -33.554 | -33.552 | -33.553 | -33.552 | -33.548 | -33.55 | -33.544 | -33.539 | -33.534 | -33.522 | -33.514 | -33.501 | -33.485 | -33.466 | -33.444 | -33.42 | -33.393 | -33.366 | -33.335 | -33.3 | -33.263 | -33.223
Split line | -30.643 | -30.757 | -30.494 | -29.68 | -28.521 | -27.326 | -26.193 | -24.955 | -23.719 | -22.554 | -21.346 | -20.236 | -19.175 | -18.18 | -17.239 | -16.222 | -15.278 | -14.401 | -13.552 | -12.741 | -11.995 | -11.207 | -10.365 | -9.497 | -8.695
Cover center(inner) | -30.494 | -30.544 | -30.289 | -29.75 | -29.13 | -28.231 | -27.344 | -26.322 | -25.315 | -24.332 | -23.479 | -22.626 | -21.843 | -21.105 | -20.403 | -19.641 | -18.899 | -18.121 | -17.417 | -16.794 | -16.18 | -15.605 | -14.996 | -14.349 | -13.737
Cover center(outer) | -30.286 | -25.304 | -18.663 | -19.325 | -17.044 | -16.153 | -14.438 | -12.632 | -14.746 | -14.12 | -12.59 | -12.123 | -12.317 | -10.308 | -9.722 | -8.445 | -8.604 | -9.304 | -7.926 | -7.778 | -6.581 | -5.629 | -5.193 | -4.852 | -5.246
Note: Five thermal couples (106,107,108,109,110) are not used.

## Slide 12: Result & analysis KC-2
Chart: 
DAB Center(TR) | -33.83 | -33.827 | -33.828 | -33.828 | -33.826 | -33.819 | -33.81 | -33.792 | -33.771 | -33.742 | -33.706 | -33.663 | -33.615 | -33.56 | -33.498 | -33.433 | -33.361 | -33.284 | -33.202 | -33.118 | -33.03 | -32.937 | -32.846 | -32.748 | -32.649
Tearline Root(inner) | -31.328 | -31.132 | -30.963 | -30.614 | -29.938 | -29.066 | -28.114 | -27.204 | -26.314 | -25.438 | -24.514 | -23.65 | -22.782 | -21.933 | -21.097 | -20.268 | -19.398 | -18.603 | -17.822 | -17.072 | -16.395 | -15.713 | -14.962 | -14.234 | -13.551
Cover center(inner) | -30.634 | -30.481 | -30.742 | -30.558 | -30.241 | -29.726 | -29.12 | -28.508 | -27.85 | -27.168 | -26.5 | -25.827 | -25.142 | -24.449 | -23.811 | -23.146 | -22.475 | -21.871 | -21.247 | -20.64 | -20.03 | -19.478 | -18.902 | -18.319 | -17.775
Cover center(outer) | -30.703 | -21.934 | -15.517 | -10.887 | -10.486 | -10.093 | -9.32 | -8.341 | -8.043 | -6.922 | -6.228 | -5.836 | -5.773 | -5.27 | -4.815 | -4.436 | -4.456 | -3.902 | -4.397 | -3.378 | -3.081 | -2.529 | -2.226 | -2.193 | -1.297
DAB Center(TC) | -30.705 | -30.714 | -30.734 | -30.717 | -30.714 | -30.714 | -30.728 | -30.72 | -30.731 | -30.72 | -30.725 | -30.717 | -30.714 | -30.72 | -30.72 | -30.708 | -30.699 | -30.687 | -30.664 | -30.643 | -30.626 | -30.594 | -30.576 | -30.564 | -30.515
Inflator Bottom (outer) | -31.023 | -29.781 | -27.106 | -24.316 | -22.267 | -20.969 | -19.862 | -19.154 | -18.564 | -18.058 | -17.606 | -17.341 | -17.17 | -17.074 | -16.94 | -16.502 | -16.351 | -16.161 | -16.263 | -16.365 | -16.138 | -15.834 | -15.62 | -15.444 | -15.103
Tearline w/o emblem (inner) | -30.456 | -30.456 | -30.415 | -30.193 | -29.83 | -29.303 | -28.697 | -28.044 | -27.406 | -26.727 | -26.056 | -25.371 | -24.675 | -23.991 | -23.306 | -22.627 | -21.939 | -21.283 | -20.629 | -19.953 | -19.337 | -18.716 | -18.08 | -17.479 | -16.89
Infltor bottom(inner) | -31.185 | -31.226 | -30.881 | -30.869 | -30.72 | -30.497 | -30.213 | -29.897 | -29.552 | -29.13 | -28.671 | -28.202 | -27.722 | -27.213 | -26.677 | -26.133 | -25.579 | -25.073 | -24.52 | -23.991 | -23.494 | -22.991 | -22.502 | -22.008 | -21.508
Tearline w emblem root(outer) | -30.227 | -27.82 | -22.935 | -19.001 | -15.933 | -13.593 | -11.676 | -10.046 | -8.971 | -7.916 | -7.119 | -6.86 | -6.454 | -5.967 | -5.382 | -4.853 | -4.255 | -3.77 | -3.362 | -3.09 | -2.788 | -2.488 | -2.125 | -1.794 | -1.398
Chart: 
DAB Center(TR) | 82.6 | 82.6 | 82.594 | 82.6 | 82.597 | 82.597 | 82.597 | 82.594 | 82.588 | 82.582 | 82.568 | 82.565 | 82.548 | 82.53 | 82.513 | 82.49 | 82.464 | 82.432 | 82.406 | 82.368 | 82.337 | 82.293 | 82.25 | 82.209 | 82.166
Tearline Root(inner) | 81.851 | 82.012 | 81.921 | 81.811 | 81.364 | 80.724 | 80.1 | 79.55 | 79.006 | 78.474 | 77.951 | 77.382 | 76.854 | 76.364 | 75.866 | 75.362 | 74.874 | 74.41 | 73.957 | 73.513 | 73.055 | 72.632 | 72.19 | 71.715 | 71.268
Cover center(inner) | 81.429 | 81.394 | 81.406 | 81.406 | 81.353 | 81.235 | 81.085 | 80.842 | 80.595 | 80.322 | 80.025 | 79.702 | 79.373 | 79.013 | 78.666 | 78.297 | 77.945 | 77.595 | 77.232 | 76.874 | 76.524 | 76.173 | 75.869 | 75.517 | 75.17
Cover center(outer) | 81.548 | 79.125 | 74.058 | 70.602 | 69.96 | 69.544 | 68.836 | 67.621 | 66.308 | 65.16 | 64.122 | 64.621 | 64.361 | 63.189 | 63.475 | 63.032 | 63.03 | 62.696 | 62.001 | 61.961 | 61.302 | 60.86 | 59.225 | 58.868 | 59.446
DAB Center(TC) | 81.649 | 81.535 | 81.625 | 81.663 | 81.668 | 81.657 | 81.67 | 81.67 | 81.673 | 81.663 | 81.676 | 81.67 | 81.67 | 81.66 | 81.663 | 81.639 | 81.647 | 81.636 | 81.617 | 81.631 | 81.639 | 81.61 | 81.596 | 81.583 | 81.575
Inflator Bottom (outer) | 82.091 | 81.346 | 79.993 | 78.371 | 77.112 | 76.273 | 75.538 | 74.799 | 74.147 | 73.553 | 73.041 | 72.829 | 72.712 | 72.559 | 72.272 | 72.11 | 71.938 | 71.948 | 71.826 | 71.718 | 71.676 | 71.456 | 71.28 | 71.169 | 71.068
Tearline w/o emblem (inner) | 81.68 | 81.656 | 81.747 | 81.668 | 81.561 | 81.325 | 81.012 | 80.653 | 80.243 | 79.813 | 79.339 | 78.848 | 78.302 | 77.767 | 77.21 | 76.651 | 76.108 | 75.559 | 75.04 | 74.505 | 73.987 | 73.459 | 72.947 | 72.456 | 71.935
Infltor bottom(inner) | 82.328 | 82.045 | 82.244 | 82.15 | 82.09 | 81.979 | 81.859 | 81.707 | 81.532 | 81.325 | 81.095 | 80.88 | 80.607 | 80.361 | 80.077 | 79.801 | 79.52 | 79.245 | 78.958 | 78.665 | 78.372 | 78.072 | 77.767 | 77.47 | 77.156
Tearline w emblem root(outer) | 81.958 | 65.416 | 58.266 | 59.262 | 61.765 | 63.384 | 64.259 | 64.599 | 64.374 | 63.822 | 63.674 | 63.528 | 63.066 | 62.47 | 62.21 | 61.942 | 61.632 | 61.303 | 60.894 | 60.521 | 60.092 | 59.725 | 59.308 | 58.949 | 58.537

## Slide 13: Result & analysis G95
Chart: 
DAB Center(TR) | -34.309 | -34.309 | -34.309 | -34.306 | -34.305 | -34.299 | -34.29 | -34.28 | -34.262 | -34.244 | -34.22 | -34.194 | -34.164 | -34.131 | -34.094 | -34.052 | -34.01 | -33.962 | -33.912 | -33.857 | -33.801 | -33.74 | -33.679 | -33.612 | -33.542
Tearline Root(inner) | -31.125 | -30.507 | -30.185 | -29.541 | -28.552 | -27.326 | -26.048 | -24.654 | -23.162 | -21.616 | -20.362 | -19.038 | -18.017 | -16.924 | -16.016 | -15.196 | -14.136 | -13.221 | -12.509 | -11.67 | -10.828 | -10.056 | -9.24 | -8.545 | -7.976
Cover center(inner) | -30.878 | -30.989 | -30.907 | -30.816 | -30.761 | -30.705 | -30.618 | -30.526 | -30.428 | -30.264 | -30.084 | -29.879 | -29.655 | -29.399 | -29.135 | -28.887 | -28.597 | -28.296 | -27.999 | -27.706 | -27.374 | -27.063 | -26.765 | -26.476 | -26.164
Cover center(outer) | -30.015 | -21.333 | -16.539 | -15.785 | -13.933 | -10.89 | -11.373 | -9.707 | -9.591 | -8.12 | -7.41 | -6.19 | -6.971 | -6.266 | -6.507 | -5.828 | -5.407 | -4.694 | -4.258 | -3.134 | -2.793 | -2.549 | -2.244 | -1.376 | -1.594
DAB Center(TC) | -30.919 | -30.886 | -30.802 | -30.802 | -30.816 | -30.804 | -30.801 | -30.797 | -30.79 | -30.773 | -30.737 | -30.673 | -30.626 | -30.547 | -30.486 | -30.43 | -30.366 | -30.275 | -30.175 | -30.076 | -29.979 | -29.868 | -29.8 | -29.694 | -29.589
Inflator Bottom (outer) | -31.19 | -29.878 | -27.568 | -25.865 | -24.714 | -24.088 | -23.291 | -22.932 | -22.649 | -22.551 | -22.311 | -21.895 | -21.374 | -20.86 | -20.363 | -20.167 | -20.12 | -20.358 | -20.364 | -20.237 | -20.527 | -20.897 | -20.71 | -19.993 | -19.811
Tearline w/o emblem (inner) | -30.868 | -30.458 | -30.358 | -30.265 | -30.022 | -29.868 | -29.724 | -29.535 | -29.411 | -29.148 | -28.805 | -28.372 | -28.146 | -27.697 | -27.527 | -27.237 | -26.757 | -26.451 | -26.177 | -25.855 | -25.558 | -25.249 | -24.802 | -24.389 | -24.235
Infltor bottom(inner) | -31.086 | -30.922 | -30.854 | -30.822 | -30.734 | -30.642 | -30.551 | -30.416 | -30.304 | -30.131 | -29.957 | -29.799 | -29.572 | -29.389 | -29.149 | -28.963 | -28.721 | -28.478 | -28.227 | -27.999 | -27.754 | -27.519 | -27.27 | -27.023 | -26.786
Tearline w emblem root(outer) | -30.504 | -25.114 | -13.446 | -11.183 | -10.471 | -8.553 | -7.084 | -5.246 | -4.233 | -3.49 | -3.897 | -4.26 | -4.176 | -3.763 | -2.825 | -1.489 | -1.313 | -1.496 | -1.3 | -0.479 | -0.07 | 0.089 | -0.059 | -0.425 | 0.26
Chart: 
DAB Center(TR) | 82.501 | 82.499 | 82.504 | 82.496 | 82.487 | 82.478 | 82.464 | 82.447 | 82.426 | 82.418 | 82.409 | 82.392 | 82.383 | 82.366 | 82.354 | 82.331 | 82.311 | 82.285 | 82.259 | 82.233 | 82.201 | 82.169 | 82.14 | 82.102 | 82.073
Tearline Root(inner) | 82.218 | 82.247 | 82.195 | 82.125 | 81.987 | 81.81 | 81.537 | 81.119 | 80.125 | 79.931 | 79.358 | 78.73 | 78.148 | 77.325 | 76.66 | 75.816 | 75.112 | 74.397 | 73.632 | 72.787 | 72.032 | 71.524 | 70.675 | 69.79 | 68.999
Cover center(inner) | 81.682 | 81.714 | 81.698 | 81.658 | 81.648 | 81.614 | 81.558 | 81.411 | 81.381 | 81.366 | 81.284 | 81.242 | 81.175 | 81.112 | 81.022 | 80.933 | 80.837 | 80.744 | 80.625 | 80.492 | 80.374 | 80.208 | 80.07 | 79.866 | 79.697
Cover center(outer) | 82.363 | 39.595 | 64.34 | 69.724 | 47.323 | 41.381 | 62.784 | 63.113 | 64.956 | 55.589 | 56.453 | 48.149 | 47.948 | 46.851 | 44.855 | 50.406 | 52.593 | 53.283 | 37.947 | 32.87 | 31.897 | 26.9 | 26.396 | 27.701 | 26.231
DAB Center(TC) | 81.407 | 81.415 | 81.366 | 81.337 | 81.323 | 81.304 | 81.259 | 81.188 | 81.159 | 81.119 | 81.114 | 81.088 | 81.085 | 81.059 | 80.998 | 80.99 | 80.953 | 80.9 | 80.871 | 80.836 | 80.767 | 80.73 | 80.688 | 80.614 | 80.561
Inflator Bottom (outer) | 81.961 | 81.826 | 81.164 | 80.362 | 79.827 | 79.449 | 79.131 | 78.306 | 77.273 | 76.655 | 76.251 | 75.957 | 75.792 | 75.646 | 75.368 | 75.174 | 75.231 | 75.109 | 74.946 | 74.904 | 74.827 | 74.516 | 74.407 | 74.307 | 74.194
Tearline w/o emblem (inner) | 82.001 | 81.993 | 81.953 | 81.887 | 81.827 | 81.671 | 81.529 | 81.294 | 81.165 | 81.02 | 80.867 | 80.711 | 80.556 | 80.349 | 80.164 | 79.991 | 79.815 | 79.661 | 79.486 | 79.302 | 79.097 | 78.864 | 78.599 | 78.377 | 78.147
Infltor bottom(inner) | 81.84 | 81.785 | 81.703 | 81.635 | 81.578 | 81.522 | 81.387 | 81.224 | 81.152 | 81.072 | 80.973 | 80.896 | 80.784 | 80.666 | 80.571 | 80.442 | 80.292 | 80.159 | 80.028 | 79.876 | 79.724 | 79.578 | 79.403 | 79.259 | 79.115
Tearline w emblem root(outer) | 82.803 | 79.562 | 69.859 | 66.338 | 65.23 | 64.735 | 63.789 | 57.562 | 56.614 | 55.708 | 53.812 | 54.449 | 55.186 | 51.237 | 50.277 | 49.884 | 52.615 | 42.338 | 38.065 | 34.974 | 32.605 | 31.202 | 29.89 | 29.239 | 28.134

## Slide 14: Result & analysis P3011
Chart: 
DAB Center(TR) | -33.388 | -33.39 | -33.387 | -33.388 | -33.386 | -33.389 | -33.386 | -33.385 | -33.383 | -33.382 | -33.375 | -33.371 | -33.361 | -33.351 | -33.339 | -33.322 | -33.307 | -33.285 | -33.266 | -33.24 | -33.213 | -33.184 | -33.155 | -33.12 | -33.085
Tearline Root(inner) | -29.107 | -29.18 | -29.069 | -28.93 | -28.565 | -28.14 | -27.67 | -27.235 | -26.752 | -26.288 | -25.835 | -25.4 | -24.988 | -24.521 | -24.11 | -23.728 | -23.268 | -22.827 | -22.389 | -21.924 | -21.456 | -20.964 | -20.493 | -20.036 | -19.584
Cover center(inner) | -29.706 | -29.565 | -29.539 | -29.31 | -28.93 | -28.453 | -27.942 | -27.454 | -26.9 | -26.396 | -25.867 | -25.339 | -24.842 | -24.324 | -23.802 | -23.332 | -22.82 | -22.356 | -21.863 | -21.386 | -20.907 | -20.459 | -19.985 | -19.551 | -19.108
Cover center(outer) | -29.373 | -26.393 | -18.777 | -16.754 | -14.911 | -13.533 | -12.624 | -11.832 | -11.329 | -11.048 | -10.654 | -10.634 | -9.702 | -9.427 | -8.839 | -8.057 | -7.479 | -7.227 | -7.357 | -7.092 | -6.609 | -6.49 | -6.325 | -6.12 | -5.745
DAB Center(TC) | -30.168 | -30.098 | -29.998 | -30.077 | -30.048 | -30.06 | -30.051 | -30.053 | -30.088 | -30.088 | -30.093 | -30.111 | -30.11 | -30.099 | -30.087 | -30.096 | -30.075 | -30.098 | -30.072 | -30.09 | -30.058 | -30.043 | -30.028 | -30.017 | -29.991
Inflator Bottom (outer) | -30.469 | -30.495 | -30.355 | -30.234 | -30.111 | -29.899 | -29.568 | -29.152 | -28.65 | -28.18 | -27.647 | -27.121 | -26.648 | -26.282 | -25.978 | -25.768 | -25.639 | -25.545 | -25.434 | -25.244 | -25.019 | -24.779 | -24.406 | -24.042 | -23.668
Tearline w/o emblem (inner) | -28.771 | -28.706 | -28.61 | -28.608 | -28.504 | -28.28 | -28.005 | -27.682 | -27.329 | -26.934 | -26.525 | -26.142 | -25.692 | -25.253 | -24.798 | -24.357 | -23.929 | -23.495 | -23.082 | -22.614 | -22.146 | -21.672 | -21.189 | -20.718 | -20.211
Infltor bottom(inner) | -30.614 | -30.048 | -27.159 | -24.944 | -23.331 | -21.763 | -20.264 | -19.036 | -18.179 | -17.119 | -16.139 | -15.732 | -15.254 | -14.947 | -14.694 | -14.529 | -14.259 | -13.984 | -13.806 | -13.655 | -13.468 | -12.933 | -12.322 | -12.123 | -11.947
Tearline w emblem root(outer) | -28.773 | -27.031 | -23.181 | -19.442 | -17.419 | -15.981 | -14.899 | -14.14 | -13.462 | -12.917 | -12.532 | -12.089 | -11.584 | -11.078 | -10.541 | -9.804 | -9.298 | -8.844 | -8.41 | -7.932 | -7.429 | -7.128 | -6.974 | -6.667 | -6.32
Chart: 
DAB Center(TR) | 82.143 | 82.149 | 82.146 | 82.149 | 82.152 | 82.152 | 82.154 | 82.154 | 82.149 | 82.152 | 82.152 | 82.157 | 82.149 | 82.146 | 82.14 | 82.134 | 82.123 | 82.117 | 82.108 | 82.097 | 82.085 | 82.068 | 82.053 | 82.033 | 82.013
Tearline Root(inner) | 81.645 | 81.677 | 81.602 | 81.528 | 81.218 | 80.745 | 80.246 | 79.753 | 79.297 | 78.833 | 78.413 | 78.044 | 77.667 | 77.307 | 76.965 | 76.593 | 76.259 | 75.959 | 75.623 | 75.31 | 75.01 | 74.722 | 74.419 | 74.096 | 73.805
Cover center(inner) | 81.337 | 81.4 | 81.35 | 81.281 | 81.079 | 80.747 | 80.359 | 79.941 | 79.532 | 79.051 | 78.6 | 78.131 | 77.706 | 77.242 | 76.828 | 76.366 | 75.934 | 75.46 | 75.07 | 74.667 | 74.249 | 73.832 | 73.403 | 73.035 | 72.655
Cover center(outer) | 81.623 | 79.495 | 68.956 | 70.635 | 64.567 | 66.538 | 67.245 | 66.171 | 65.495 | 65.353 | 65.038 | 63.977 | 63.239 | 62.701 | 61.656 | 61.69 | 62.624 | 61.043 | 60.324 | 59.67 | 59.974 | 59.625 | 58.684 | 58.079 | 57.535
DAB Center(TC) | 81.25 | 81.268 | 81.194 | 81.213 | 81.239 | 81.226 | 81.213 | 81.229 | 81.235 | 81.23 | 81.201 | 81.212 | 81.204 | 81.199 | 81.212 | 81.199 | 81.194 | 81.186 | 81.175 | 81.167 | 81.167 | 81.17 | 81.165 | 81.159 | 81.125
Inflator Bottom (outer) | 81.959 | 81.957 | 81.951 | 81.904 | 81.766 | 81.61 | 81.44 | 81.268 | 81.072 | 80.827 | 80.638 | 80.429 | 80.156 | 79.912 | 79.658 | 79.337 | 79.078 | 78.831 | 78.614 | 78.386 | 78.16 | 77.97 | 77.758 | 77.519 | 77.243
Tearline w/o emblem (inner) | 81.321 | 81.388 | 81.356 | 81.348 | 81.26 | 81.103 | 80.875 | 80.592 | 80.324 | 79.968 | 79.652 | 79.294 | 78.94 | 78.574 | 78.203 | 77.822 | 77.419 | 77.077 | 76.709 | 76.314 | 75.951 | 75.598 | 75.264 | 74.92 | 74.575
Infltor bottom(inner) | 82.392 | 81.568 | 80.523 | 78.684 | 76.768 | 75.6 | 74.8 | 73.835 | 72.913 | 72.343 | 71.894 | 71.308 | 70.707 | 70.33 | 69.776 | 69.353 | 69.239 | 69.133 | 68.923 | 68.695 | 68.65 | 68.488 | 68.064 | 67.64 | 67.321
Tearline w emblem root(outer) | 81.858 | 79.926 | 74.572 | 71.319 | 67.558 | 67.875 | 68.051 | 67.733 | 67.593 | 67.43 | 67.396 | 67.085 | 66.702 | 66.339 | 65.859 | 65.523 | 65.433 | 65.309 | 65.149 | 64.866 | 64.444 | 64.035 | 63.646 | 63.211 | 62.81

## Slide 15: Result & analysis
Channel | Location | SX12 |  |  |  |  |  | KC-2 |  |  |  |  |  | Dongfeng G95 |  |  |  |  |  | Changcheng P3011 |  |  |  |  | 
 |  | 85℃ |  |  | -35℃ |  |  | 85℃ |  |  | -35℃ |  |  | 85℃ |  |  | -35℃ |  |  | 85℃ |  |  | -35℃ |  | 
 |  | 0s | 120s | Diff. | 0s | 120s | Diff. | 0s | 120s | Diff. | 0s | 120s | Diff. | 0s | 120s | Diff. | 0s | 120s | Diff. | 0s | 120s | Diff. | 0s | 120s | Diff.
101 | DAB center | 82.814 | 82.715 | 0.099 | -33.552 | -33.223 | -0.329 | 82.6 | 82.166 | 0.434 | -33.83 | -32.649 | -1.181 | 82.501 | 82.073 | 0.428 | -34.309 | -33.542 | -0.767 | 82.143 | 82.013 | 0.13 | -33.388 | -33.085 | -0.303
103 | Tearline root (inner) | 82.238 | 76.61 | 5.628 | -30.643 | -8.695 | -21.948 | 81.851 | 71.268 | 10.583 | -31.328 | -13.551 | -17.777 | 82.218 | 68.999 | 13.219 | -31.125 | -7.976 | -23.149 | 81.645 | 73.805 | 7.84 | -29.107 | -19.584 | -9.523
104 | Cover center(inner) | 81.871 | 70.434 | 11.437 | -30.494 | -13.737 | -16.757 | 81.429 | 75.17 | 6.259 | -30.634 | -17.775 | -12.859 | 81.682 | 79.697 | 1.985 | -30.878 | -26.164 | -4.714 | 81.337 | 72.655 | 8.682 | -29.706 | -19.108 | -10.598
105 | Cover center(outer) | 81.755 | 59.6 | 22.155 | -30.286 | -5.246 | -25.04 | 81.548 | 59.446 | 22.102 | -30.703 | -1.297 | -29.406 | 82.363 | 26.231 | 56.132 | -30.015 | -1.594 | -28.421 | 81.623 | 57.535 | 24.088 | -29.373 | -5.745 | -23.628
106 | DAB Center(TC) |  | \ |  |  | \ |  | 81.649 | 81.575 | 0.074 | -30.705 | -30.515 | -0.19 | 81.407 | 80.561 | 0.846 | -30.919 | -29.589 | -1.33 | 81.25 | 81.125 | 0.125 | -30.168 | -29.991 | -0.177
107 | Inflator Bottom (outer) |  | \ |  |  | \ |  | 82.091 | 71.068 | 11.023 | -31.023 | -15.103 | -15.92 | 81.961 | 74.194 | 7.767 | -31.19 | -19.811 | -11.379 | 81.959 | 77.243 | 4.716 | -30.469 | -23.668 | -6.801
108 | Tearline w/o emblem (inner) |  | \ |  |  | \ |  | 81.68 | 71.935 | 9.745 | -30.456 | -16.89 | -13.566 | 82.001 | 78.147 | 3.854 | -30.868 | -24.235 | -6.633 | 81.321 | 74.575 | 6.746 | -28.771 | -20.211 | -8.56
109 | Infltor bottom(inner) |  | \ |  |  | \ |  | 82.328 | 77.156 | 5.172 | -31.185 | -21.508 | -9.677 | 81.84 | 79.115 | 2.725 | -31.086 | -26.786 | -4.3 | 82.392 | 67.321 | 15.071 | -30.614 | -11.947 | -18.667
110 | Tearline w emblem root(outer)） |  | \ |  |  | \ |  | 81.958 | 58.537 | 23.421 | -30.227 | -1.398 | -28.829 | 82.803 | 28.134 | 54.669 | -30.504 | 0.26 | -30.764 | 81.858 | 62.81 | 19.048 | -28.773 | -6.32 | -22.453

## Slide 16
Chart: 
| DAB center | Tearline root (inner) | Cover center(inner) | Cover center(outer)
 | -0.099 | -5.628 | -11.437 | -22.155
Chart: 
| DAB center | Tearline root (inner) | Cover center(inner) | Cover center(outer)
 | 0.329 | 21.948 | 16.757 | 25.04
DAB Module – SX12 Housing: PG8 PA6 40% fiber Design type: Floating module

## Slide 17: DAB Module – KC-2 Housing: Steel Design type: Floating module
Chart: 
| DAB center | Tearline root (inner) | Cover center(inner) | Cover center(outer) | DAB Center(TC) | Inflator Bottom (outer) | Tearline w/o emblem (inner) | Infltor bottom(inner) | Tearline w emblem root(outer)）
 | -0.434 | -10.583 | -6.259 | -22.102 | -0.074 | -11.023 | -9.745 | -5.172 | -23.421
Chart: 
| DAB center | Tearline root (inner) | Cover center(inner) | Cover center(outer) | DAB Center(TC) | Inflator Bottom (outer) | Tearline w/o emblem (inner) | Infltor bottom(inner) | Tearline w emblem root(outer)）
 | 1.181 | 17.777 | 12.859 | 29.406 | 0.19 | 15.92 | 13.566 | 9.677 | 28.829

## Slide 18: DAB Module – G95 Housing: PG8 PA6 40% fiber Design type: Floating cover
Chart: 
| DAB center | Tearline root (inner) | Cover center(inner) | Cover center(outer) | DAB Center(TC) | Inflator Bottom (outer) | Tearline w/o emblem (inner) | Infltor bottom(inner) | Tearline w emblem root(outer)）
 | -0.428 | -13.219 | -1.985 | -56.132 | -0.846 | -7.767 | -3.854 | -2.725 | -54.669
Chart: 
| DAB center | Tearline root (inner) | Cover center(inner) | Cover center(outer) | DAB Center(TC) | Inflator Bottom (outer) | Tearline w/o emblem (inner) | Infltor bottom(inner) | Tearline w emblem root(outer)）
 | 0.767 | 23.149 | 4.714 | 28.421 | 1.33 | 11.379 | 6.633 | 4.3 | 30.764

## Slide 19: DAB Module – P3011 Housing: Steel Design type: Floating module
Chart: 
| DAB center | Tearline root (inner) | Cover center(inner) | Cover center(outer) | DAB Center(TC) | Inflator Bottom (outer) | Tearline w/o emblem (inner) | Infltor bottom(inner) | Tearline w emblem root(outer)）
 | -0.13 | -7.84 | -8.682 | -24.088 | -0.125 | -4.716 | -6.746 | -15.071 | -19.048
Chart: 
| DAB center | Tearline root (inner) | Cover center(inner) | Cover center(outer) | DAB Center(TC) | Inflator Bottom (outer) | Tearline w/o emblem (inner) | Infltor bottom(inner) | Tearline w emblem root(outer)）
 | 0.303 | 9.523 | 10.598 | 23.628 | 0.177 | 6.801 | 8.56 | 18.667 | 22.453

## Slide 20: Result & analysis -- -35℃
Chart: 
| DAB center | Tearline root (inner) | Cover center(inner) | Cover center(outer) | DAB Center(TC) | Inflator Bottom (outer) | Tearline w/o emblem (inner) | Infltor bottom(inner) | Tearline w emblem root(outer)）
 | 1.181 | 17.777 | 12.859 | 29.406 | 0.19 | 15.92 | 13.566 | 9.677 | 28.829
 | 0.767 | 23.149 | 4.714 | 28.421 | 1.33 | 11.379 | 6.633 | 4.3 | 30.764
 | 0.303 | 9.523 | 10.598 | 23.628 | 0.177 | 6.801 | 8.56 | 18.667 | 22.453
 | 0.329 | 21.948 | 16.757 | 25.04
KC-2
G95
P3011
SX12
SX12
KC-2
P3011
G95
27
25
0.5
0.5
11
11
18
9
11

## Slide 21: Conclusion The setting temperature is -35℃, but actually the initial temperature is about -30 ℃, and the mean temperature rise range from 26.93 to 0.65 from outer to inner.
 | Mean Initial Temperature/℃ | Mean 2 min. Temperature/℃ | Mean temperature rise/℃
Outer surface | -29.98 | -3.05 | 26.93
Inner surface | -30.49 | -17.73 | 12.77
DAB center | TC: -30.60 | -30.03 | 0.57
 | TR: -33.77 | -33.12 | 0.65
Note：TC-Thermal couple，TR: Thermal Resistance

## Slide 22: Result & analysis -- 85℃
Chart: 
| DAB center | Tearline root (inner) | Cover center(inner) | Cover center(outer) | DAB Center(TC) | Inflator Bottom (outer) | Tearline w/o emblem (inner) | Infltor bottom(inner) | Tearline w emblem root(outer)）
 | -0.434 | -10.583 | -6.259 | -22.102 | -0.074 | -11.023 | -9.745 | -5.172 | -23.421
 | -0.428 | -13.219 | -1.985 | -56.132 | -0.846 | -7.767 | -3.854 | -2.725 | -54.669
 | -0.13 | -7.84 | -8.682 | -24.088 | -0.125 | -4.716 | -6.746 | -15.071 | -19.048
 | -0.099 | -5.628 | -11.437 | -22.155
KC-2
G95
P3011
SX12
SX12
KC-2
P3011
G95
TC separate from cover
TC separate from cover
-23
-21
-9
-7.5
-7
-7.5
-7
0
0

## Slide 23: Conclusion The setting temperature is 85℃, but actually the initial temperature is about 81℃, and the mean temperature decrease range from 26.93 to 0.65 from outer to inner.
 | Mean Initial Temperature/℃ | Mean 2 min. Temperature/℃ | Mean temperature decrease/℃
Outer surface | 81.75 | 59.59 | -22.16
Inner surface | 81.85 | 74.06 | -7.78
DAB center | TC: 81.44 | 54.00 | -10.36
 | TR: 82.51 | 82.24 | -0.273
Note：TC-Thermal couple，TR: Thermal Resistance

## Slide 24: Temperature differences source
1
2
3
4
Maybe the volume of DAB chamber and airbag folded type influent the temperature distribution
DAB temperature cannot attain its simulation temperature.
DAB temperature distribution is not uniform，especially for cover.
DAB temperature change rate is influenced by the environment temperature and heat convection.

## Slide 25: Test defect
1. The thermal couples are pasted on the surface of DAB, so the inner temperature of cover along the thickness cannot be collected, maybe the temperature change rate is not greater than surface.
2. Maybe the temperature along the tear line change rate is greater because its thickness is less than the DAB average thickness, but the thermal couples cannot pasted in the tear line.
3.Actually, before the DAB deployment test, the DAB module will be transfered mounted on the test equipment in 2 min. So maybe the temperature change rate is greater than this test.

## Slide 26: Temperature influence on mechanical property of polymer
(Ref. An Introduction to the Mechanical Properties of Solid Polymers)

## Slide 27: TA4003BE – 30°C
Ductile failure

## Slide 28: TA4003BE – RT
Necking and cold drawing

## Slide 29: 10000mmps

## Slide 30: TA4003BE – 85°C
Homogeneous defromation